## Slide 1
FD04 Frangibolt Performance Test for SunRISE: Measuring Force and Stroke Margin
SunRISE
Ingie Baho, Kim Aaron
5/2023

## Slide 2: Table of Contents
Introduction
Background
Test Parameters
Test Materials
MGSE Configuration
Procedure
Results
Conclusions and Discussion
Acknowledgements
This document has been reviewed and determined not to contain export controlled technical data.

## Slide 3: Introduction
This presentation proposes a new standard test method to measure the performance of FD04 Frangibolt actuators. Performance is quantified in terms of force and stroke required to break a bolt restraining the deployable.
Other Frangibolt models have been tested using a method which is not appropriate for the FD04 given the nature of the crystal structure of the shape memory alloy (SMA).
The novelty of this test procedure is that an initial pre-load is applied to the Frangibolt before actuation which simulates the load a torqued bolt in a flight assembly would apply.
Overview
Motivation
Novelty
This document has been reviewed and determined not to contain export controlled technical data.
Notes: -explain how Frangibolts are used: HDRM

## Slide 4: Background (1/2): SunRISE Frangibolts
A Frangibolt is a release mechanism used in small satellites which is easily resettable, non-explosive, and low-cost manufactured by Ensign-Bickford Aerospace & Defense (EBAD)
Hardware:
  Shape memory alloy (SMA) which undergoes phase transition (martensite to austenite)
  Heater element
  Resistance temperature detector (RTD)
Test campaign was conducted for Sun Radio Interferometer Space Experiment (SunRISE):
  Boom antennas restrained/deployed with FD04 Frangibolts
This document has been reviewed and determined not to contain export controlled technical data.
Notes: Talking points:
What a frangibolt is: it’s been increasingly used in small sats, made by EBAD
Introduce hardware: single crystal SMA (as opposed to multiple crystal), explain redundancy and RTD, wrapped in silicon insulating layer
Explain how it works and reference video – describe force and stroke
Describe what sunRISE is: The SunRISE mission aims to launch an array of six CubeSats to collectively monitor solar activity to better understand solar particle storms [2]. A key payload of the CubeSats is the Spiral Tube Actuator for Controlled Extension / Retraction (STACER) antenna, which is a boom that is restrained and deployed using Frangibolt actuators. 6 cubesats are flying in geosynchronous orbit facing the sun
What type of heating element is in the Frangibolt
Martensite: a hard and very brittle solid solution of carbon in iron that is the main constituent of hardened steel
Austenite: a solid solution of carbon in a nonmagnetic form of iron, stable at high temperatures. It is a constituent of some forms of steel.

## Slide 5: Background (2/2): Frangibolt Testing
Instron initially applies full test load to Frangibolt
Frangibolt is then actuated, and the stroke is recorded
The FC model Frangibolts have multi-crystal SMA, and the grain boundaries provide nucleation sites for phase change, even at high loads
Frangibolt
Instron Platens
Previous Approach
Current Approach
FC Frangibolt (Polycrystalline)
FD Frangibolt (Monocrystalline)
Potential nucleation sites
Instron Platen
Frangibolt
Fixtures designed to apply pre-load
The FD Frangibolts have a single crystal SMA and no grain boundaries to facilitate nucleation
A small pre-load must first be applied before actuation, allowing a nucleation site to form
Once the actuator begins undergoing phase transition, then the load applied to the Frangibolt may be ramped up
This document has been reviewed and determined not to contain export controlled technical data.
Notes: Say what an Instron does: it applies a force and measures displacement, which in this case is the expansion of the Frangibolt, or stroke

## Slide 6: Test Parameters
Performance of the Frangibolt is quantified in terms:
Force Margin: Amount of force the Frangibolt can produce beyond what is needed to break the fastener
  SunRISE requirement: 100%
Stroke Margin: Amount of stroke the Frangibolt undergoes beyond what is needed to break the fastener
  SunRISE requirement: 10%
Frangibolt Specifications:
  Bolt-breaking Force: 622-643 lbf
  Bolt-breaking Stroke: ~0.008 in
  Bolt Pre-load: 150 lbf
This document has been reviewed and determined not to contain export controlled technical data.
Notes: Explain bolt preload and JPL DPs

## Slide 7: Test Materials
Test Units:
  2 FD04 Frangibolts from the SunRISE flight lot (F1942, F1943)
  2 FR-4 thermal insulation washers
  Mechanical Ground Support Equipment:
  McMaster Belleville washers (9712K459) (x2)
  Belleville washer cup
  Top and bottom Frangibolt fixtures
  Stabilizing posts (x3)
  McMaster-Carr spring plunger tips (3126A2) (x3)
  Spacer blocks (x3)
Electrical Ground Support Equipment:
  Agilent 34980 data acquisition system (DAQ)
  Keysight N5765A power supply
Testing Machines/Metrology:
  Instron 8801 Servo-hydraulic Fatigue Testing System (with 25kN load cell)
  Epsilon Axial Extensometer (Model 3542)
This document has been reviewed and determined not to contain export controlled technical data.
Notes: Only present the extensometer: describe what an extensometer is - An extensometer is a device that is used to measure changes in the length of an object. It is useful for stress-strain measurements and tensile tests. Its name comes from "extension-meter"

## Slide 8: Mechanical Ground Support Equipment
McMaster PN: 9712K459
Washers were selected to approximately match the stiffness of the fastener
Fastener stiffness: 88914.26 lbf/in
Washer stack stiffness: 85000 lbf/in
Belleville Washers (x2)
Belleville Washer Cup
Spacers (x3) (third one removed for visualization)
Top and Bottom Frangibolt Fixture
Bottom Instron Platen
Top Instron Platen
FD04 Frangibolt
FR-4 Washers (x2)
Stabilizing posts (x3)
This document has been reviewed and determined not to contain export controlled technical data.
Notes: Missing stabilizing posts,
What’s the point of the springs : The spring plunger tips were adjusted to ensure that the washer cup sat parallel to the plane of the Instron platen (horizontal). Instron platen has not been lowered yet. This is the starting position of the set-up, but the test has not yet started. During test, the spring plunger force is small enough to be negligible. Their compressed length is such that they do not bottom out.
Explain the significance of the spring plungers not being bottomed out before the test starts
Explain what a Belleville washer is: a deformed washer that acts as a spring
call out the stabilizing post which holds the cup level and prevents tipping

## Slide 9: Procedure (1/5)
~0.002” gap
The Instron platen was lowered until it just barely touches the top Belleville washer
There is a small gap between the Instron platen and the spacer blocks (~0.002”)
1. Before Test Begins
This document has been reviewed and determined not to contain export controlled technical data.

## Slide 10: Procedure (2/5)
2. Applying 150 lbf Pre-load
The Instron was programmed to increase load to desired test load
The Instron platen lowered until it hit the stiff spacer blocks, compressing the Bellevilles and apply 150 lbf to the Frangibolt
Test Loads | Force (lbf)
Min Bolt Breaking Load | 622
Max Bolt Breaking Load | 643
1.3x Max Bolt Breaking Load | 836
1.5x Max Bolt Breaking Load | 965
2.0x Max Bolt Breaking Load | 1286
This document has been reviewed and determined not to contain export controlled technical data.
Notes: Intron was in force controlled, meaning when we program the force, the instonr lowers and keeps applying load until programmed load is attained
Load is programmed to linearly increase,
After Instron hits spacers, and the force applied by the Instron continues to increase, all the remaining force goes through spacer block.
Note: This is equivalent to installing the Frangibolt with the fastener pre-loaded to 150 lbf.
Explain different test loads in the table and where they come from

## Slide 11: Procedure (3/5)
3. Actuating Frangibolt
Once the test load was attained, 5.5V was applied to the Frangibolt
The expanding Frangibolt compressed the Belleville washers up against the Instron platen such that the load on the Frangibolt was increasing and the load on the spacers was decreasing
This document has been reviewed and determined not to contain export controlled technical data.
Notes: This is equivalent to the Frangibolt expanding and applying more load on the fastener, but it hasn’t broken the bolt yet.
Belleville washers compressed by Instron platen (note: washer cup does not touch Instron platen. All the central force goes through the Belleville washers to the Frangibolt.)

## Slide 12: Procedure (4/5)
The Frangibolt expands until it pushes the Instron platen off the spacer
At this point, the Frangibolt is carrying the entire test load applied by the Instron and is still expanding
4. Frangibolt Expands
This document has been reviewed and determined not to contain export controlled technical data.
Notes: The point when the Instron platen is pushed off the spacers is equivalent to the Frangibolt breaking the bolt, as it has demonstrated enough stroke at the test load (643 lbf). All the additional expansion after this point is considered margin. Include flight version of what’s happening

## Slide 13: Procedure (5/5)
The power was turned off when Frangibolt reached 180°C
The Frangibolt was removed from the fixture, compressed using the reset tool, and placed back into the Instron to be tested at next test load
5. Frangibolt Reset
Top Instron platen is lowered onto the assembly
Top Instron platen has been moved away
Reset Tool
This document has been reviewed and determined not to contain export controlled technical data.
Notes: -180 is do not exceed temp defined by EBAD
-

## Slide 14: Results (1/2): Calculation of Stroke Margin
Calculation of Stroke Margin:
Using values from the plot:
Power on
Power off
Bolt-breaking Stroke = 0.008in
Stroke Margin
Actuator Stroke Available = 0.0381 in
Note: This test load is equivalent to max bolt breaking load, therefore, force margin = 0
This document has been reviewed and determined not to contain export controlled technical data.

## Slide 15: Results (2/2): Calculation of Force Margin
Max Bolt-breaking Load = 643 lbf
Force Margin
Test Load = 1286 lbf
Calculation of Force Margin:
Using values from the plot:
Note: In the higher test loads, the Frangibolt exhibited additional stroke while the Instron was unloading. This additional stroke was not included in the stroke margin calculations.
This document has been reviewed and determined not to contain export controlled technical data.

## Slide 16: Conclusions and Discussion
For the two Frangibolts tested at the maximum force of 1286 lbf, which corresponds to 100% force margin, the average stroke margin was 28%
  Our test method qualified the SunRISE flight lot of 24 Frangibolts + spares
Future work:
  The MGSE can be resized so to accommodate different Frangibolt models and sizes
  The Belleville washers can be selected to match the stiffness of a different notched fastener
We’d like to propose this method as a new standard for qualifying flight Frangibolts, which currently does not exist in the literature
  The test was repeatable and yielded the results that were needed
  This new approach could be used for Frangibolts with any SMA crystalline structure, but the older approach could only be used for polycrystalline structure SMAs
When the previous test method was used, our Frangibolts appeared to not work. However, with our method, we discovered that the Frangibolts actually exceeded performance requirements.
This document has been reviewed and determined not to contain export controlled technical data.

## Slide 17: Acknowledgements
The research was carried out at the Jet Propulsion Laboratory, California Institute of Technology, under a contract with the National Aeronautics and Space Administration (80NM0018D0004). We would like to acknowledge the SunRISE project at the Jet Propulsion Laboratory for funding this work.