## Slide 1
Nicolas Gross, Athip Thirupathi Raj, Jekan Thangavelautham
Space and Terrestrial Robotic Exploration (SpaceTREx) Laboratory
Aerospace and Mechanical Engineering Department
University of Arizona
Shape Memory Alloy Based Hard Docking Mechanisms for two-stage CubeSat Docking

## Slide 2: Outline
Introduction and Motivation
Related Work
Objectives
Methodology
Design
Results and Discussion
Conclusions and Future Work

## Slide 3: Introduction and Motivation
Current methods for docking are large-scale and require manual controls
For CubeSats: electromagnetic soft docking is being developed
Hard docking: creates physical lock, prevents separation between satellites
Two-stage docking of CubeSats could allow for in-space assembly, on-orbit servicing and transfer of goods(i.e., fuel, data, samples)
Electromagnetic soft docking1
Robotic space station via in-space assembly

## Slide 4: Related Work
Androgynous Peripheral Attach System (APAS)
  Can assume both passive and active role
  Guide pins, active latches, passive catches
  Spring-loaded separation system
  Soyuz, Space Shuttle, Mir, ISS, SpaceX Dragon
NASA Docking System
  Low Impact Docking System (LIDS)
  Evolution of APAS
  Minimized impact forces when docking with force-sensing and active control technology
  Hard docking mechanisms remained the same
Diagram of APAS-758
NASA Docking System Test7
Notes: APAS: ring holding guides(pins) shifts to align the active unit latches with the passive unit catches, then shock absorbers dissipate residual impact energy, active unit then retracts to bring them closer together, four-spring push rods drive spacecraft away during undocking, APAS-75 was the first, also 89 and 95
LIDS: very similar to APAS, made to be compatible with APAS, capable of docking and berthing, real-time performance adjustment and configurability, in terms of hard docking, the mechanisms are almost identical to Russian APAS: latches and hooks catch, spring-load separation device is now retractable

## Slide 5: Related Work
Several complex probe and cone prototypes for Small Sats in development, but none have been tested in space
Modified cone and probe adapters optimize geometry for simplicity
Probe and drogue, University of Padova3
ARCADE docking render4
SpaceTREx modified cone and probe adapters5
Modified adapters soft docking demo

## Slide 6: Objectives
System Requirements:
  Successful automatic lock after soft docking phase
  Remain locked: resist forces (magnitude TBD)
  Able to unlock upon command
  Fit within 1U form factor
Optimizations:
  Minimize time required to lock/unlock
  Minimize the mass/volume taken by the entire latch mechanism
Change the current modified cone and probe adapters to include a hard docking mechanism with the following requirements and optimizations:
Sectioned docking assembly

## Slide 7: Methodology: System Architecture
Docking System
Modified Cone
Curved Groove
Modified Probe
Hinge
Flap
SMA Springs

## Slide 8: Concept of Operations
Phase 3: Hard Capture
Launch
Deploy Runner
Deploy Chaser
Phase 1: Initial Rendezvous
Phase 2: Soft Capture
Phase 4: Release and Decommission

## Slide 9: Introduction to SMA
How does SMA work?
  Transitions from martensite phase at low temperatures to austenite phase at high temperatures through shape memory effect (SME)
  One-Way (OWSME): after deformation at low temperature, SMA returns to original trained shape
  Two-Way (TWSME): SMA has two trained states, one at low temperatures and one at high temperatures
Advantages
  High force to weight ratio, low cost
How does this fit into the hard docking model?
  TWSME spring actuates latch
  Low temperature: extended (lock)
  High temperature: compressed (unlock)
SMA phase change loop6
Notes: Add labels to image

## Slide 10: Design
Modified Cone
Curved Groove
Modified Probe
SMA Spring
Hinge
Modified cone(left) and modified probe(right)
Spring Interface

## Slide 11: Interfacing
Progression of spring interface prototypes from left to right
Telescopic cylinders prototypes
Spring interfaces between hinge and modified probe
  Must keep spring fixed on each end while allowing for actuation
Because SMA is elastic, springs bend laterally
  To avoid lateral deflection, restrict movement with telescopic cylinder

## Slide 12: SMA Spring Characterization
Perform spring testing to determine:
  deflection under load
  deflection after actuation
  current/temperature required for actuation
  response time
  cycle time
Test multiple spring with different spring parameters and different loadings

## Slide 13: Testing Facility
Test apparatus consists of 3D printed frame and circuit to deliver current to springs
Spring attached to top of frame with weight attached to bottom
Arduino relay setup
  control current output and time
Camera in the front and ruler in the back for deflection measurement
Develop different setup for compression spring testing
Test Frame
SMA Spring
Measuring Ruler
Calibrated Weight
Power Supply
Relay
Camera
Thermometer
Complete test setup

## Slide 14: Results and Discussion
Current adapters with SMA springs can lock and unlock successfully
Challenges with interfacing
OWSME vs TWSME SMA springs
TWSME Spring9
Notes: Add labels to image

## Slide 15: Conclusions and Future Work
Complete testing of SMA springs
Integrate adapters into 1U frames
Print adapters in metal
Further iterate design (SMA in cone)
Full docking assembly
1U Frame
Modified Cone
Modified Probe
1U metal assembly

## Slide 16: Questions?

## Slide 17
Space and Terrestrial Robotic Exploration (SpaceTREx) Laboratory

## Slide 18: References
1Duzzi, Matteo, et al. “GNC 2017.” ELECTROMAGNETIC POSITION AND ATTITUDE CONTROL FOR PACMAN EXPERIMENT, May 2017, https://www.researchgate.net/publication/317369805_ELECTROMAGNETIC_POSITION_AND_ATTITUDE_CONTROL_FOR_PACMAN_EXPERIMENT.
2Thangavelautham, J., & Thirupathi Raj, A. (October 2021). Active Lighting and Cues to Facilitate Cooperative On-Orbit Two-Stage Docking by Small Satellites. 72th International Astronautical Congress. Dubai: International Astronautical Federation.
3Branz, Francesco, et al. “Miniature Docking Mechanism for CubeSats.” Acta Astronautica, vol. 176, 2020, pp. 510–519., https://doi.org/10.1016/j.actaastro.2020.06.042
4Boesso, A., and A. Francesconi. “Arcade Small-Scale Docking Mechanism for Micro-Satellites.” Acta Astronautica, vol. 86, 2013, pp. 77–87., https://doi.org/10.1016/j.actaastro.2013.01.006
5Raj, A. T., Sturgeon, C., & Thangavelautham, J. (2022). Optimization of Geometric Mating Pairs for Small Spacecraft Docking.
6Sonawane, Nikhil. “Precision Pointing in Space Using Arrays of Shape Memory Based Linear Actuators.”
7Parma, G. (2011). AIAA Annual Technical Symposium, https://web.archive.org/web/20111015075220/http://dockingstandard.nasa.gov/Documents/AIAA_ATS_NDS-IDSS_Overview_Draft1.pdf.
8Androgynous peripheral attach system. Academic Dictionaries and Encyclopedias. (2010), https://en-academic.com/dic.nsf/enwiki/2294545
9YouTube. (2020, May 19). Nitinol Kellogg's Research Labs. YouTube, https://www.youtube.com/watch?v=9O8PcaFDWvs&ab_channel=Kellogg%27sResearchLabs-Nitinol